Injection in SIMsalabim:
including roughness
L. Jan Anton Koster
Zernike Institute for Advanced Materials
University of Groningen

---
Outline
- Injection model:
  - image-force-lowering
  - Scott&Malliaras
- Effect of roughness
  - enhanced field
  - enhanced injection
- SIMsalabim:
  - implementation

---
Injection model
- Many different models exist...
- Use a simple one: Scott & Malliaras*
- Due to image force lowering, the carrier density at (close really) the electrode equals (eq. 11 in paper):
- where:
- S&M also give a formula for the current, but we don't need it as we can only use 1 formula (either for n or J).
*Scott&Malliaras, Chem. Phys. Lett. 199, 115 (1999)
see also: Di Carlo et al., Org. Elec. 15, 1557 (2014).
n_0=4 \psi^2 N_c \exp\left( -\frac{\phi_b+\sqrt{f}}{kT}\right)
f=qFr_c/kT

---
Roughness
- George has shown that roughness at the electrode can enhance injection (the field, really)*
- Injection current is exponential in the field => to get the average current, we need cannot simply insert the average field in the S&M formula.
- George's formula for Schottky emission reads:
- Note: very similar to S&M's formula for n (previous slide)
*G. Palasantzas et al., Phys. Rev. B 60, 9157 (1999)
J_sc = A_S T^2 \exp\left( -\frac{\phi_b-\beta \sqrt{F}}{kT} \right)

---
Roughness
- Enhanced injection current (Schottky emission) due to roughness:
- F2 is the second-order term in the Taylor series that George uses. We will calculate it later
- This means that the carrier density in the S&M model is given by:
- where we assume that ψ does not change due to roughness.
G. Palasantzas et al., Phys. Rev. B 60, 9157 (1999)
\frac{J_{sc}}{J_{sc}^0} = \exp\left( \frac{\beta\sqrt{F_0}}{2kT} \frac{F_2}{F_0} \right )
\frac{n_0^{\rm rough} }{n_0}= \exp\left( \frac{\beta\sqrt{F_0}}{2kT} \frac{F_2}{F_0} \right )

---
Roughness: calculating the field
- Use George's eq. 31:
- Δ=w/h0. w=rms roughness, h0=film thickness
- a=0.5 approximately. This is calculated from the roughness parameters (i.e. input from Solmaz)
- L=ξ/h0. ξ=lateral correlation length, ~100 nm.
- α=0.5-0.7: roughness exponent. Lower value means more spiky surface.
G. Palasantzas et al., Phys. Rev. B 60, 9157 (1999)
\frac{F_2}{F_0}=\Delta^2 L^2 \int_0^{q_c} \frac{ q^2 \coth q}{ (1+aL^2 q^2)^{1+\alpha}} dq

---
SIMsalabim: implementation
- There are two effects (formulae shown in previous slides)
  - image-force lowering
  - roughness which enhances injection
- The S&M equation (w or w/o roughness) for n0 (carrier density at electrode) means that we can calculate the barrier lowering by assuming Boltzmann statistics.
- Note: we need Boltzmann statistics at the contacts (V,n,p) to ensure that J=0 if V=0.
- So: in every iteration, we adjust V(0) and n(0), p(0).
  - so use law of mass action to get minority density
- Note: F2/F0 is constant during the simulation, so it can be computed externally.

---
SIMsalabim: implementation
- What about the sign of F0?
- lowering term only used if it really lowers the barrier, otherwise just use phi_b (=input value).